# Calculated Raman spectra of MB⁺: comparison of free molecule and flat adsorption on Ag₄₀

Comparison based on the three supplied TmoleX/TURBOMOLE Excel exports

# 1. Overlay of calculated spectra

For comparability, the original (ort,unpol) line intensities between 500 and 1800 cm⁻¹ were normalized separately to 100 %. The overlay below uses the same Gaussian broadening (σ = 8 cm⁻¹) for all three data sets. Thus, peak positions and relative intensity patterns can be compared directly; absolute intensities are not compared.

Figure 1. Calculated Raman spectra, normalized within 500–1800 cm⁻¹.

# 2. Tabular comparison

| Spectral region | MB⁺ no COSMO /cm⁻¹ | MB⁺ COSMO geometry /cm⁻¹ | MB⁺/Ag₄₀ flat /cm⁻¹ | Observation |
| --- | --- | --- | --- | --- |
| Main high-frequency band | 1638.35 | 1639.12 | 1626.04 | Ag: red shift ≈ 12–13 cm⁻¹ |
| ~1530 cm⁻¹ region | 1530.50 | 1537.51 | 1501.86* | Ag: marked intensity redistribution |
| ~1490 cm⁻¹ region | 1486.09 | 1490.22 | 1490–1502* | Position broadly retained |
| ~1450 cm⁻¹ region | 1447.71 | 1447.25 | near 1450* | Small frequency change |
| ~1370–1380 cm⁻¹ region | 1377.20 | 1378.88 | 1366.28 / 1370.44 | Ag: red shift / splitting |
| ~1150 cm⁻¹ region | 1149.06 | 1150.67 | 1164.85 | Ag: blue shift ≈ 14–16 cm⁻¹ |
| ~950 cm⁻¹ region | 948.77 | 948.46 | near 940–950* | Moderate change |

*For the Ag₄₀ system, several regions contain multiple modes and strongly redistributed intensities; entries marked with an asterisk are therefore spectral-region comparisons rather than one-to-one mode assignments.

# 3. Main findings

The dominant high-frequency Raman band of free MB⁺ occurs at 1638.35 cm⁻¹ (no COSMO) and 1639.12 cm⁻¹ (COSMO-optimized geometry). In the flat MB⁺/Ag₄₀ structure it occurs at 1626.04 cm⁻¹, corresponding to a red shift of about 12–13 cm⁻¹.

The free-molecule spectra are similar in their principal peak positions. The COSMO-optimized geometry therefore changes the characteristic Raman frequencies only modestly in comparison with adsorption on silver.

Adsorption on Ag₄₀ causes a pronounced redistribution of relative Raman intensity. In the 500–800 cm⁻¹ region, the Ag-containing calculation shows strong contributions at 578.88, 593.18, 707.82 and 788.75 cm⁻¹ that are much more prominent than in the free-molecule spectra.

A further clear change is seen near 1150 cm⁻¹: 1149.06/1150.67 cm⁻¹ for free MB⁺ versus 1164.85 cm⁻¹ for the flat Ag₄₀ configuration.

The changes are consistent with a substantial perturbation of the molecular vibrational/polarizability response upon interaction with the Ag cluster. They should not, by themselves, be interpreted as a quantitative classical SERS enhancement factor, because the calculation does not establish the experimental electromagnetic enhancement or molecule-number normalization.

# 4. Interpretation for the SERS comparison

The most useful comparison with the experimental SERS spectrum is therefore not the absolute calculated intensity but (i) the positions of characteristic MB⁺ bands, (ii) adsorption-induced frequency shifts, and (iii) changes in the relative intensity pattern. The calculated red shift of the high-frequency band to 1626.04 cm⁻¹ and the strong redistribution in the 500–800 cm⁻¹ region are particularly diagnostic features of the flat MB⁺/Ag₄₀ model.